## Slide 1: FATIGUE
Endurance Limit Modifying Factors

## Slide 2: Cumulative Damage Log-Log Plot For Test Sample
103
104
105
106
0.9 Sut
S’e
Cycles, N
Stress
σ3
σ2
σ1
N1
N2
N3
n1
σ – Cyclic Stress Level
n – Number of Cycles
S’f – Fatigue Strength at N
N – Number of Cycles to Failure given S’f
S’e - Endurance Limit
Sut- Ultimate Strength

## Slide 3: Endurance Limit Modifying Factors
Se=kakbkckdkekfS’e
  ka-surface factor
  kb-size factor
  kc-reliability factor
  kd-temperature factor
  ke-modifying factor for stress concentrations
  kf-miscellaneous effects factor

## Slide 4: ka – Surface factor

## Slide 5: kb – Size Effect
Rotating beam test specimen is 0.3 in in diameter
Large specimens
  2in dia -> 10 to 25% reduction in Se
  Dia > 2in -> 25% reduction
For bending and torsion, kb
  d≤0.3in (7.6mm) -> kb=1
  0.3≤d≤2.0 -> kb=0.85
  d>2.0in -> kb=0.75
For Axial loading, kb=1

## Slide 6: kc- Loading Factor
Bending kc=1
Axial kc=0.85
Torsion kc=0.59

## Slide 7: kd - Temperature
For steel
  T < 160 °F -> kd=1
  T > 160 °F -> kd=620/(460+T)

## Slide 8: Stress Concentration
Kt – theoretical or geometric static stress concentration factor
Kf – fatigue strength reduction factor
  (endurance limit of notch free specimen)/(endurance limit of notched specimens)
  Kf =1+q(Kt-1), q-notch sensitivity
  ke=1/Kf

## Slide 9: Stress Concentration
Kt – theoretical or geometric static stress concentration factor
Kf – fatigue strength reduction factor
Notch Sensitivity Factor

## Slide 10: Neuber Constants,
Steel Loaded in Tension
Annealed Aluminum
Hardened Aluminum
Sut (ksi) | 15 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90
Sut (Msi) | 103 | 138 | 207 | 276 | 345 | 414 | 483 | 552 | 621
 | 0.175 | 0.380 | 0.278 | 0.219 | 0.186 | 0.162 | 0.144 | 0.131 | 0.122
Sut (ksi) | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45
Sut (Msi) | 69 | 103 | 138 | 172 | 207 | 241 | 276 | 310
 | 0.500 | 0.341 | 0.264 | 0.217 | 0.180 | 0.152 | 0.123 | 0.111
Sut (ksi) | 50 | 60 | 70 | 80 | 90 | 100 | 120 | 140 | 160 | 180 | 200 | 220 | 240
Sut (Msi) | 345 | 414 | 483 | 552 | 621 | 689 | 827 | 965 | 1103 | 1241 | 1379 | 1517 | 1655
 | 0.130 | 0.108 | 0.093 | 0.080 | 0.070 | 0.062 | 0.049 | 0.039 | 0.031 | 0.024 | 0.018 | 0.013 | 0.009

## Slide 11: Notch Sensitivity Curves

## Slide 12: Additional Notch Sensitivity Curves

## Slide 13: ke - Reliability
Reliability, R | Standardized Variable, zR | kc
0.50 | 0 | 1.000
0.90 | 1.288 | 0.897
0.95 | 1.645 | 0.868
0.99 | 2.326 | 0.814
0.999 | 3.091 | 0.753
0.999 9 | 3.719 | 0.702
0.999 99 | 4.265 | 0.659
0.999 999 | 4.753 | 0.620
0.999 999 9 | 5.199 | 0.584
0.999 999 99 | 5.612 | 0.551
0.999 999 999 | 5.997 | 0.520

## Slide 14: Example
A rotating shaft is supported by ball bearings at A and D and loaded by the non-rotating force F. Estimate the life of this part.
Sut=103ksi
Syt=72ksi
Shaft is drawn
UNS G10350 steel, drawn at 1000 C
Machined finish
10 in
3 in
4 in
5 in
1500 lb
0.5 in
0.5 in
1.18 in
1.25 in
1. 50 in
1.375 in
1.18 in
A
B
C
D
All Fillets 1/8 in Radius
M