## Slide 1
Chapter 6
Fatigue Failure Resulting from Variable Loading
Lecture Slides
© 2015 by McGraw-Hill Education. This is proprietary material solely for authorized instructor use. Not authorized for sale or distribution in any manner. This document may not be copied, scanned, duplicated, forwarded, distributed, or posted on a website, in whole or part.

## Slide 2: Chapter Outline

## Slide 3: Introduction to Fatigue in Metals
Loading produces stresses that are variable, repeated, alternating, or fluctuating
Maximum stresses well below yield strength
Failure occurs after many stress cycles
Failure is by sudden ultimate fracture
No visible warning in advance of failure

## Slide 4: Stages of Fatigue Failure
Stage I – Initiation of micro-crack due to cyclic plastic deformation
Stage II – Progresses to macro-crack that repeatedly opens and closes, creating bands called beach marks
Stage III – Crack has propagated far enough that remaining material is insufficient to carry the load, and fails by simple ultimate failure
Fig. 6–1
From ASM Handbook,
Vol. 12: Fractography, 2nd
printing, 1992, ASM International,
Materials Park, OH
44073-0002, fig 50, p. 120.
Reprinted by permission
of ASM International®,
www.asminternational.org.)

## Slide 5: Schematics of Fatigue Fracture Surfaces
Fig. 6–2
From ASM Metals
Handbook, Vol. 11: Failure
Analysis and Prevention, 1986,
ASM International, Materials
Park, OH 44073-0002, fig 18,
p. 111. Reprinted by permission
of ASM International®,
www.asminternational.org.

## Slide 6: Schematics of Fatigue Fracture Surfaces
Fig. 6–2
From ASM Metals
Handbook, Vol. 11: Failure
Analysis and Prevention, 1986,
ASM International, Materials
Park, OH 44073-0002, fig 18,
p. 111. Reprinted by permission
of ASM International®,
www.asminternational.org.

## Slide 7: Schematics of Fatigue Fracture Surfaces
Fig. 6–2
From ASM Metals
Handbook, Vol. 11: Failure
Analysis and Prevention, 1986,
ASM International, Materials
Park, OH 44073-0002, fig 18,
p. 111. Reprinted by permission
of ASM International®,
www.asminternational.org.

## Slide 8: Fatigue Fracture Examples
AISI 4320 drive shaft
B– crack initiation at stress concentration in keyway
C– Final brittle failure
Fig. 6–3
From ASM Handbook,
Vol. 12: Fractography,
2nd printing, 1992, ASM
International, Materials
Park, OH 44073-0002, fig 51,
p. 120. Reprinted by permission
of ASM International®,
www.asminternational.org.

## Slide 9: Fatigue Fracture Examples
Fatigue failure initiating at mismatched grease holes
Sharp corners (at arrows) provided stress concentrations
Fig. 6–4
From ASM Handbook,
Vol. 12: Fractography,
2nd printing, 1992, ASM
International, Materials Park,
OH 44073-0002, fig 520,
p. 331. Reprinted by permission
of ASM International®,
www.asminternational.org

## Slide 10: Fatigue Fracture Examples
Fatigue failure of forged connecting rod
Crack initiated at flash line of the forging at the left edge of picture
Beach marks show crack propagation halfway around the hole before ultimate fracture
Fig. 6–5
From ASM Handbook,
Vol. 12: Fractography,
2nd printing, 1992, ASM
International, Materials Park,
OH 44073-0002, fig 523,
p. 332. Reprinted by permission
of ASM International®,
www.asminternational.org.)

## Slide 11: Fatigue Fracture Examples
Fatigue failure of a 200-mm diameter piston rod of an alloy steel steam hammer
Loaded axially
Crack initiated at a forging flake internal to the part
Internal crack grew outward symmetrically
Fig. 6–6
(From ASM Handbook, Vol. 12: Fractography, 2nd printing, 1992, ASM
International, Materials Park, OH 44073-0002, fig 570, p. 342. Reprinted
by permission of ASM International®, www.asminternational.org.)

## Slide 12: Fatigue Fracture Examples
Double-flange trailer wheel
Cracks initiated at stamp marks
Fig. 6–7
From ASM Metals Handbook, Vol. 11: Failure Analysis and Prevention, 1986, ASM International, Materials Park, OH
44073-0002, fig 51, p. 130. Reprinted by permission of ASM International®, www.asminternational.org.

## Slide 13: Fatigue Fracture Examples
Aluminum allow landing-gear torque-arm assembly redesign to eliminate fatigue fracture at lubrication hole
Fig. 6–8
From ASM Metals Handbook, Vol. 11: Failure Analysis and Prevention, 1986, ASM International, Materials Park, OH 44073-0002, fig 23, p. 114. Reprinted by permission of ASM International®, www.asminternational.org

## Slide 14: Fatigue-Life Methods
Three major fatigue life models
Methods predict life in number of cycles to failure, N, for a specific level of loading
Stress-life method
  Least accurate, particularly for low cycle applications
  Most traditional, easiest to implement
Strain-life method
  Detailed analysis of plastic deformation at localized regions
  Several idealizations are compounded, leading to uncertainties in results
Linear-elastic fracture mechanics method
  Assumes crack exists
  Predicts crack growth with respect to stress intensity

## Slide 15: Stress-Life Method
Test specimens are subjected to repeated stress while counting cycles to failure
Most common test machine is R. R. Moore high-speed rotating-beam machine
Subjects specimen to pure bending with no transverse shear
As specimen rotates, stress fluctuates between equal magnitudes of tension and compression, known as completely reversed stress cycling
Specimen is carefully machined and polished
Fig. 6–9

## Slide 16: S-N Diagram
Number of cycles to failure at varying stress levels is plotted on log-log scale
For steels, a knee occurs near 106 cycles
Strength corresponding to the knee is called endurance limit Se
Fig. 6–10

## Slide 17: S-N Diagram for Steel
Stress levels below Se predict infinite life
Between 103 and 106 cycles, finite life is predicted
Below 103 cycles is known as low cycle, and is often considered quasi-static. Yielding usually occurs before fatigue in this zone.
Fig. 6–10

## Slide 18: S-N Diagram for Nonferrous Metals
Nonferrous metals often do not have an endurance limit.
Fatigue strength Sf is reported at a specific number of cycles
Figure 6–11 shows typical S-N diagram for aluminums
Fig. 6–11

## Slide 19: Strain-Life Method
  Method uses detailed analysis of plastic deformation at localized regions
Compounding of several idealizations leads to significant uncertainties in numerical results
Useful for explaining nature of fatigue

## Slide 20: Strain-Life Method
  Fatigue failure almost always begins at a local discontinuity
  When stress at discontinuity exceeds elastic limit, plastic strain occurs
  Cyclic plastic strain can change elastic limit, leading to fatigue
  Fig. 6–12 shows true stress-true strain hysteresis loops of the first five stress reversals
Fig. 6–12

## Slide 21: Relation of Fatigue Life to Strain
Figure 6–13 plots relationship of fatigue life to true-strain amplitude
Fatigue ductility coefficient e'F is true strain corresponding to fracture in one reversal (point A in Fig. 6–12)
Fatigue strength coefficient s'F is true stress corresponding to fracture in one reversal (point A in Fig. 6–12)
Fig. 6–13

## Slide 22: Relation of Fatigue Life to Strain
Fatigue ductility exponent c is the slope of plastic-strain line, and is the power to which the life 2N must be raised to be proportional to the true plastic-strain amplitude. Note that 2N stress reversals corresponds to N cycles.
Fatigue strength exponent b is the slope of the elastic-strain line, and is the power to which the life 2N must be raised to be proportional to the true-stress amplitude.
Fig. 6–13

## Slide 23: Relation of Fatigue Life to Strain
Total strain is sum of elastic and plastic strain
Total strain amplitude is half the total strain range
The equation of the plastic-strain line in Fig. 6–13
The equation of the elastic strain line in Fig. 6–13
Applying Eq. (a), the total-strain amplitude is

## Slide 24: Relation of Fatigue Life to Strain
Known as Manson-Coffin relationship between fatigue life and total strain
Some values of coefficients and exponents given in Table A–23
Equation has limited use for design since values for total strain at discontinuities are not readily available

## Slide 25: Linear-Elastic Fracture Mechanics Method
  Assumes Stage I fatigue (crack initiation) has occurred
  Predicts crack growth in Stage II with respect to stress intensity
  Stage III ultimate fracture occurs when the stress intensity factor KI reaches some critical level KIc

## Slide 26: Crack Growth
Stress intensity factor is given by
For a stress range Ds, the stress intensity range per cycle is
Testing specimens at various levels of Ds provide plots of crack length vs. stress cycles
Fig. 6–14

## Slide 27: Crack Growth
Log-log plot of rate of crack growth, da/dN, shows all three stages of growth
Stage II data are linear on log-log scale
Similar curves can be generated by changing the stress ratio R = smin/ smax
Fig. 6–15

## Slide 28: Crack Growth
Crack growth in Region II is approximated by the Paris equation
C and m are empirical material constants. Conservative representative values are shown in Table 6–1.

## Slide 29: Crack Growth
Substituting Eq. (6–4) into Eq. (6–5) and integrating,
ai is the initial crack length
af is the final crack length corresponding to failure
Nf is the estimated number of cycles to produce a failure after the initial crack is formed

## Slide 30: Crack Growth
If b is not constant, then the following numerical integration algorithm can be used.

## Slide 31: Example 6–1
Fig. 6–16

## Slide 32: Example 6–1 (continued)

## Slide 33: Example 6–1 (continued)
Fig. 5–27

## Slide 34: Example 6–1 (continued)

## Slide 35: The Endurance Limit
The endurance limit for steels has been experimentally found to be related to the ultimate strength
Fig. 6–17

## Slide 36: The Endurance Limit
Simplified estimate of endurance limit for steels for the rotating-beam specimen, S'e
Fig. 6–17

## Slide 37: Fatigue Strength
For design, an approximation of the idealized S-N diagram is desirable.
To estimate the fatigue strength at 103 cycles, start with Eq. (6–2)
Define the specimen fatigue strength at a specific number of cycles as
Combine with Eq. (6–2),

## Slide 38: Fatigue Strength
At 103 cycles,
f is the fraction of Sut represented by
Solving for f,
The SAE approximation for steels with HB ≤ 500 may be used.
To find b, substitute the endurance strength and corresponding cycles into Eq. (6–9) and solve for b

## Slide 39: Fatigue Strength
Eqs. (6–11) and (6–12) can be substituted into Eqs. (6–9) and (6–10) to obtain expressions for S'f and f

## Slide 40: Fatigue Strength Fraction f
Plot Eq. (6–10) for the fatigue strength fraction f of Sut at 103 cycles
Use f from plot for S'f = f Sut at 103 cycles on S-N diagram
Assumes Se = S'e= 0.5Sut at 106 cycles
Fig. 6–18

## Slide 41: Equations for S-N Diagram
Write equation for S-N line from 103 to 106 cycles
Two known points
At N =103 cycles, Sf = f Sut
At N =106 cycles, Sf = Se
Equations for line:
Fig. 6–10

## Slide 42: Equations for S-N Diagram
If a completely reversed stress srev is given, setting Sf = srev in Eq. (6–13) and solving for N gives,
Note that the typical S-N diagram is only applicable for completely reversed stresses
For other stress situations, a completely reversed stress with the same life expectancy must be used on the S-N diagram

## Slide 43: Low-cycle Fatigue
Low-cycle fatigue is defined for fatigue failures in the range 1 ≤ N ≤ 103
On the idealized S-N diagram on a log-log scale, failure is predicted by a straight line between two points (103, f Sut) and (1, Sut)

## Slide 44: Example 6–2

## Slide 45: Example 6–2 (continued)

## Slide 46: Endurance Limit Modifying Factors
Endurance limit S'e is for carefully prepared and tested specimen
If warranted, Se is obtained from testing of actual parts
When testing of actual parts is not practical, a set of Marin factors are used to adjust the endurance limit

## Slide 47: Surface Factor ka
Stresses tend to be high at the surface
Surface finish has an impact on initiation of cracks at localized stress concentrations
Surface factor is a function of ultimate strength. Higher strengths are more sensitive to rough surfaces.

## Slide 48: Example 6–3

## Slide 49: Size Factor kb
Larger parts have greater surface area at high stress levels
Likelihood of crack initiation is higher
Size factor is obtained from experimental data with wide scatter
For bending and torsion loads, the trend of the size factor data is given by
Applies only for round, rotating diameter
For axial load, there is no size effect, so kb = 1

## Slide 50: Size Factor kb
For parts that are not round and rotating, an equivalent round rotating diameter is obtained.
Equate the volume of material stressed at and above 95% of the maximum stress to the same volume in the rotating-beam specimen.
Lengths cancel, so equate the areas.
For a rotating round section, the 95% stress area is the area of a ring,
Equate 95% stress area for other conditions to Eq. (6–22) and solve for d as the equivalent round rotating diameter

## Slide 51: Size Factor kb
For non-rotating round,
Equating to Eq. (6-22) and solving for equivalent diameter,
Similarly, for rectangular section h x b, A95s = 0.05 hb. Equating to Eq. (6–22),
Other common cross sections are given in Table 6–3

## Slide 52: Size Factor kb
Table 6–3
A95s for common non-rotating structural shapes

## Slide 53: Example 6–4

## Slide 54: Loading Factor kc
Accounts for changes in endurance limit for different types of fatigue loading.
Only to be used for single load types. Use Combination Loading method (Sec. 6–14) when more than one load type is present.

## Slide 55: Temperature Factor kd
Endurance limit appears to maintain same relation to ultimate strength for elevated temperatures as at room temperature
This relation is summarized in Table 6–4

## Slide 56: Temperature Factor kd
If ultimate strength is known for operating temperature, then just use that strength. Let kd = 1 and proceed as usual.
If ultimate strength is known only at room temperature, then use Table 6–4 to estimate ultimate strength at operating temperature. With that strength, let kd = 1 and proceed as usual.
Alternatively, use ultimate strength at room temperature and apply temperature factor from Table 6–4 to the endurance limit.
A fourth-order polynomial curve fit of the underlying data of Table 6–4 can be used in place of the table, if desired.

## Slide 57: Example 6–5

## Slide 58: Example 6–5 (continued)

## Slide 59: Reliability Factor ke
From Fig. 6–17, S'e = 0.5 Sut is typical of the data and represents 50% reliability.
Reliability factor adjusts to other reliabilities.
Only adjusts Fig. 6–17 assumption. Does not imply overall reliability.
Fig. 6–17

## Slide 60: Reliability Factor ke
Simply obtain ke for desired reliability from Table 6–5.
Table 6–5

## Slide 61: Miscellaneous-Effects Factor kf
Reminder to consider other possible factors.
  Residual stresses
  Directional characteristics from cold working
  Case hardening
  Corrosion
  Surface conditioning, e.g. electrolytic plating and metal spraying
  Cyclic Frequency
  Frettage Corrosion
Limited data is available.
May require research or testing.

## Slide 62: Stress Concentration and Notch Sensitivity
For dynamic loading, stress concentration effects must be applied.
Obtain Kt as usual (e.g. Appendix A–15)
For fatigue, some materials are not fully sensitive to Kt so a reduced value can be used.
Define Kf as the fatigue stress-concentration factor.
Define q as notch sensitivity, ranging from 0 (not sensitive) to 1 (fully sensitive).
For q = 0, Kf = 1
For q = 1, Kf = Kt

## Slide 63: Notch Sensitivity
Obtain q for bending or axial loading from Fig. 6–20.
Then get Kf from Eq. (6–32): Kf = 1 + q( Kt – 1)
Fig. 6–20

## Slide 64: Notch Sensitivity
Obtain qs for torsional loading from Fig. 6–21.
Then get Kfs from Eq. (6–32): Kfs = 1 + qs( Kts – 1)
Fig. 6–21

## Slide 65: Notch Sensitivity
Alternatively, can use curve fit equations for Figs. 6–20 and 6–21 to get notch sensitivity, or go directly to Kf .
Bending or axial:
Torsion:
For steels, with Sut in kpsi

## Slide 66: Notch Sensitivity for Cast Irons
Cast irons are already full of discontinuities, which are included in the strengths.
Additional notches do not add much additional harm.
Recommended to use q = 0.2 for cast irons.

## Slide 67: Example 6–6

## Slide 68: Application of Fatigue Stress Concentration Factor
Use Kf as a multiplier to increase the nominal stress.
Some designers (and previous editions of textbook) sometimes applied 1/ Kf as a Marin factor to reduce Se .
For infinite life, either method is equivalent, since
For finite life, increasing stress is more conservative. Decreasing Se applies more to high cycle than low cycle.

## Slide 69: Example 6–7

## Slide 70: Example 6–8

## Slide 71: Example 6–8 (continued)

## Slide 72: Example 6–8 (continued)

## Slide 73: Example 6–9
Fig. 6–22

## Slide 74: Example 6–9 (continued)
Fig. 6–22

## Slide 75: Example 6–9 (continued)

## Slide 76: Example 6–9 (continued)

## Slide 77: Example 6–9 (continued)

## Slide 78: Characterizing Fluctuating Stresses
The S-N diagram is applicable for completely reversed stresses
Other fluctuating stresses exist
Sinusoidal loading patterns are common, but not necessary

## Slide 79: Fluctuating Stresses
General Fluctuating
Repeated
Completely Reversed
Fig. 6–23

## Slide 80: Characterizing Fluctuating Stresses
Fluctuating stresses can often be characterized simply by the minimum and maximum stresses, smin and smax
Define sm as midrange steady component of stress (sometimes called mean stress) and sa as amplitude of alternating component of stress

## Slide 81: Characterizing Fluctuating Stresses
Other useful definitions include stress ratio
and amplitude ratio

## Slide 82: Application of Kf for Fluctuating Stresses
For fluctuating loads at points with stress concentration, the best approach is to design to avoid all localized plastic strain.
In this case, Kf should be applied to both alternating and midrange stress components.
When localized strain does occur, some methods (e.g. nominal mean stress method and residual stress method) recommend only applying Kf to the alternating stress.
The Dowling method recommends applying Kf to the alternating stress and Kfm to the mid-range stress, where Kfm is

## Slide 83: Fatigue Failure for Fluctuating Stresses
Vary the sm and sa to learn about the fatigue resistance under fluctuating loading
Three common methods of plotting results follow.

## Slide 84: Modified Goodman Diagram
Midrange stress is plotted on abscissa
All other components of stress are plotted on the ordinate
Fig. 6–24

## Slide 85: Master Fatigue Diagram
Displays four stress components as well as two stress ratios
Fig. 6–26

## Slide 86: Plot of Alternating vs Midrange Stress
Probably most common and simple to use is the plot of sa vs sm
Has gradually usurped the name of Goodman or Modified Goodman diagram
Modified Goodman line from Se to Sut is one simple representation of the limiting boundary for infinite life

## Slide 87: Plot of Alternating vs Midrange Stress
Experimental data on normalized plot of sa vs sm
Demonstrates little effect of negative midrange stress
Fig. 6–25

## Slide 88: Commonly Used Failure Criteria
Five commonly used failure criteria are shown
Gerber passes through the data
ASME-elliptic passes through data and incorporates rough yielding check
Fig. 6–27

## Slide 89: Commonly Used Failure Criteria
Modified Goodman is linear, so simple to use for design. It is more conservative than Gerber.
Soderberg provides a very conservative single check of both fatigue and yielding.
Fig. 6–27

## Slide 90: Commonly Used Failure Criteria
Langer line represents standard yield check.
It is equivalent to comparing maximum stress to yield strength.
Fig. 6–27

## Slide 91: Equations for Commonly Used Failure Criteria
Intersecting a constant slope load line with each failure criteria produces design equations
n is the design factor or factor of safety for infinite fatigue life

## Slide 92: Summarizing Tables for Failure Criteria
Tables 6–6 to 6–8 summarize the pertinent equations for Modified Goodman, Gerber, ASME-elliptic, and Langer failure criteria
The first row gives fatigue criterion
The second row gives yield criterion
The third row gives the intersection of static and fatigue criteria
The fourth row gives the equation for fatigue factor of safety
The first column gives the intersecting equations
The second column gives the coordinates of the intersection

## Slide 93: Summarizing Table for Modified Goodman

## Slide 94: Summarizing Table for Gerber

## Slide 95: Summarizing Table for ASME-Elliptic

## Slide 96: Example 6–10

## Slide 97: Example 6–10 (continued)

## Slide 98: Example 6–10 (continued)
Fig. 6–28

## Slide 99: Example 6–10 (continued)
Fig. 6–28

## Slide 100: Example 6–10 (continued)

## Slide 101: Example 6–10 (continued)
Fig. 6–29

## Slide 102: Example 6–10 (continued)

## Slide 103: Example 6–11
Fig. 6–30a

## Slide 104: Example 6–11 (continued)

## Slide 105: Example 6–11 (continued)

## Slide 106: Example 6–11 (continued)
Fig. 6–30b

## Slide 107: Example 6–11 (continued)

## Slide 108: Example 6–12

## Slide 109: Example 6–12 (continued)

## Slide 110: Example 6–12 (continued)

## Slide 111: Example 6–12 (continued)

## Slide 112: Fatigue Criteria for Brittle Materials
For many brittle materials, the first quadrant fatigue failure criteria follows a concave upward Smith-Dolan locus,
Or as a design equation,
For a radial load line of slope r, the intersection point is
In the second quadrant,

## Slide 113: Fatigue Criteria for Brittle Materials
Table A–24 gives properties of gray cast iron, including endurance limit
The endurance limit already includes ka and kb
The average kc for axial and torsional is 0.9

## Slide 114: Example 6–13
Fig. 6–31a

## Slide 115: Example 6–13 (continued)

## Slide 116: Example 6–13 (continued)

## Slide 117: Example 6–13 (continued)

## Slide 118: Example 6–13 (continued)
Fig. 6–31b

## Slide 119: Torsional Fatigue Strength
Testing has found that the steady-stress component has no effect on the endurance limit for torsional loading if the material is ductile, polished, notch-free, and cylindrical.
However, for less than perfect surfaces, the modified Goodman line is more reasonable.
For pure torsion cases, use kc = 0.59 to convert normal endurance strength to shear endurance strength.
For shear ultimate strength, recommended to use

## Slide 120: Combinations of Loading Modes
When more than one type of loading (bending, axial, torsion) exists, use the Distortion Energy theory to combine them.
Obtain von Mises stresses for both midrange and alternating components.
Apply appropriate Kf to each type of stress.
For load factor, use kc = 1. The torsional load factor (kc = 0.59) is inherently included in the von Mises equations.
If needed, axial load factor can be divided into the axial stress.

## Slide 121: Static Check for Combination Loading
Distortion Energy theory still applies for check of static yielding
Obtain von Mises stress for maximum stresses (sum of midrange and alternating)
Stress concentration factors are not necessary to check for yielding at first cycle
Alternate simple check is to obtain conservative estimate of s'max by summing s'a and s'm

## Slide 122: Example 6–14

## Slide 123: Example 6–14 (continued)

## Slide 124: Example 6–14 (continued)

## Slide 125: Example 6–14 (continued)

## Slide 126: Example 6–14 (continued)
Fig. 6–32

## Slide 127: Example 6–14 (continued)

## Slide 128: Example 6–14 (continued)

## Slide 129: Varying Fluctuating Stresses
Loading patterns may be complex
Simplifications may be necessary
Small fluctuations may be negligible compared to large cycles
Fig. 6–33

## Slide 130: Cumulative Fatigue Damage
A common situation is to load at s1 for n1 cycles, then at s2 for n2 cycles, etc.
The cycles at each stress level contributes to the fatigue damage
Accumulation of damage is represented by the Palmgren-Miner cycle-ratio summation rule, also known as Miner’s rule
  where ni is the number of cycles at stress level si and Ni is the number of cycles to failure at stress level si
c is experimentally found to be in the range 0.7 < c < 2.2, with an average value near unity
Defining D as the accumulated damage,

## Slide 131: Example 6–15
Fig. 6–33

## Slide 132: Example 6–15 (continued)

## Slide 133: Example 6–15 (continued)

## Slide 134: Example 6–15 (continued)

## Slide 135: Example 6–15 (continued)

## Slide 136: Illustration of Miner’s Rule
Figure 6–34 illustrates effect of Miner’s rule on endurance limit and fatigue failure line.
Note that the damaged material line is predicted to be parallel to original material line.
Fig. 6–34

## Slide 137: Weaknesses of Miner’s Rule
Miner’s rule fails to agree with experimental results in two ways
  It predicts the static strength Sut is damaged.
  It does not account for the order in which the stresses are applied

## Slide 138: Manson’s Method
Manson’s method overcomes deficiencies of Miner’s rule.
It assumes all fatigue lines on the S-N diagram converge to a common point at 0.9Sut at 103 cycles.
It requires each line to be constructed in the same historical order in which the stresses occur.
Fig. 6–35

## Slide 139: Surface Fatigue Strength
When two surfaces roll or roll and slide against one another, a pitting failure may occur after a certain number of cycles.
The surface fatigue mechanism is complex and not definitively understood.
Factors include Hertz stresses, number of cycles, surface finish, hardness, lubrication, and temperature

## Slide 140: Surface Fatigue Strength
From Eqs. (3–73) and (3–74), the pressure in contacting cylinders,
Converting to radius r and width w instead of length l,
Define pmax as surface endurance strength (also called contact strength, contact fatigue strength, or Hertzian endurance strength)

## Slide 141: Surface Fatigue Strength
Combining Eqs. (6–61) and (6–63),
K1 is known as Buckingham’s load-stress factor, or wear factor
In gear studies, a similar factor is used,
From Eq. (6–64), with material property terms incorporated into an elastic coefficient CP

## Slide 142: Surface Fatigue Strength
Experiments show the following relationships

## Slide 143: Surface Fatigue Strength
A longstanding correlation in steels between SC and HB at 108 cycles is
AGMA uses

## Slide 144: Surface Fatigue Strength
Incorporating design factor into Eq. (6–66),
Since this is nonlinear in its stress-load transformation, the definition of nd depends on whether load or stress is the primary consideration for failure.
If the loss of function is focused on the load,
If the loss of function is focused on the stress,