## Slide 1: FATIGUE
Finite Life/Strength
Cumulative Fatigue Damage

## Slide 2: Endurance Limit and Strength

## Slide 3: Rules of Thumb
Steel
  English Units
  Metric Units

## Slide 4: Rules of Thumb
Cast Iron
Aluminum and Magnesium

## Slide 5: Values (Reported by F.B. Stulen, H.N. Cummings, and W.C. Schulte, Preventing Fatigue Failures, Part 5, Machine Design, vol. 33, P. 161, 22 June 1961)
Material UNS No. (Alloys are heat treated, hot worked, specimens smooth, subjected to long life rotating beam test) | Tensile Strength, Sut |  | Endurance Limit, S’E |  | Standard Deviation | 
 | MPa | ksi | MPa | ksi | ksi | %
G43400 Steel | 965 1310 1580 1790 | 140 190 230 260 | 489 586 620 668 | 71 85 90 97 | 3.5 6.7 5.3 6.3 | 4.9 7.8 5.9 6.5
G43500 Steel | 2070 | 300 | 689 | 100 | 4.4 | 4.4
R50001-series Titanium Alloy | 1000 | 145 | 579 | 84 | 5.4 | 6.4
A97076 Aluminum Alloy | 524 | 76 | 186 | 27 | 1.6 | 6.0
C63000 Aluminum Bronze | 806 | 117 | 331 | 48 | 4.5 | 9.4
C17200 Beryllium Copper | 1210 | 175 | 248 | 36 | 2.7 | 7.5

## Slide 6: Finite Life, S’f, The S-N Curve

## Slide 7: Cumulative Damage Log-Log Plot
103
104
105
106
fSut
S’e
Cycles, N
Fatigue Stress
σ1
N1
n1
σ – Cyclic Stress Level
n – Number of Cycles
S’f – Fatigue Strength at N
N – Number of Cycles to Failure given S’f
S’e - Endurance Limit
Sut- Ultimate Strength

## Slide 8: Equation for the S-N Curve

## Slide 9: Example
The endurance limit of a steel member is 112MPa and the tensile strength is 385MPa. What fatigue strength corresponds to a life of 70(103) cycles.

## Slide 10: Cumulative Damage
Multiple Stress Levels
  σ1 for n1 cycles
  σ2 for n2 cycles
  Etc.
Palmgren-Miner’s Rule
  n-nubmer of cycles of stress σ applied
  N-life corresponding to σ
  C-determined experimentally
    0.7<C<2.2
    Typically C=1

## Slide 11: Example
Steel, Sut=80ksi
3000 cycles at 60ksi
How many cycles remain at 50ksi and 40ksi?
Chart: Number of Cycles
| 1000 | 10000 | 100000 | 1000000
Stress, ksi | 72 | 59.2434 | 48.7024 | 40