## Slide 1: FATIGUE
Finite Life/Strength
Cumulative Fatigue Damage

## Slide 2: Diagram of Gear Train

## Slide 3: Diagram of actual shaft

## Slide 4: Endurance Limit and Strength

## Slide 5: Rules of Thumb
Steel
  English Units
  Metric Units

## Slide 6: Rules of Thumb
Cast Iron
Aluminum and Magnesium

## Slide 7: Values (Reported by F.B. Stulen, H.N. Cummings, and W.C. Schulte, Preventing Fatigue Failures, Part 5, Machine Design, vol. 33, P. 161, 22 June 1961)
Material UNS No. (Alloys are heat treated, hot worked, specimens smooth, subjected to long life rotating beam test) | Tensile Strength, Sut |  | Endurance Limit, S’E |  | Standard Deviation | 
 | MPa | ksi | MPa | ksi | ksi | %
G43400 Steel | 965 1310 1580 1790 | 140 190 230 260 | 489 586 620 668 | 71 85 90 97 | 3.5 6.7 5.3 6.3 | 4.9 7.8 5.9 6.5
G43500 Steel | 2070 | 300 | 689 | 100 | 4.4 | 4.4
R50001-series Titanium Alloy | 1000 | 145 | 579 | 84 | 5.4 | 6.4
A97076 Aluminum Alloy | 524 | 76 | 186 | 27 | 1.6 | 6.0
C63000 Aluminum Bronze | 806 | 117 | 331 | 48 | 4.5 | 9.4
C17200 Beryllium Copper | 1210 | 175 | 248 | 36 | 2.7 | 7.5

## Slide 8: Endurance Limit Modifying Factors
Se=kakbkckdkekfS’e
  ka-surface factor
  kb-size factor
  kc-reliability factor
  kd-temperature factor
  ke-modifying factor for stress concentrations
  kf-miscellaneous effects factor

## Slide 9: ka – Surface factor

## Slide 10: kb – Size Effect
Bending and Rotating of Round Shafts
Axial Loading

## Slide 11: kb – Size Effect
Rotating beam test specimen is 0.3 in in diameter
Large specimens
  2in dia -> 10 to 25% reduction in Se
  Dia > 2in -> 25% reduction
For bending and torsion, kb
  d≤0.3in (7.6mm) -> kb=1
  0.3≤d≤2.0 -> kb=0.85
  d>2.0in -> kb=0.75

## Slide 12: kc- Loading Factor
Bending kc=1
Axial kc=0.85
Torsion
  kc=0.59 pure torsion
  kc=1.0 torsion combined with bending

## Slide 13: kd - Temperature
For steel
  T < 160 °F -> kd=1
  T > 160 °F -> kd=620/(460+T)

## Slide 14: Stress Concentration
Kt – theoretical or geometric static stress concentration factor
Kf – fatigue strength reduction factor
  (endurance limit of notch free specimen)/(endurance limit of notched specimens)
  Kf =1+q(Kt-1), q-notch sensitivity
  ke=1/Kf

## Slide 15: Stress Concentration
Kt – theoretical or geometric static stress concentration factor
Kf – fatigue strength reduction factor
Notch Sensitivity Factor

## Slide 16: Neuber Constants,
For Steel and Aluminum Reverse Bending or Reverse Axial
For Steel and Aluminum Reverse Torsion
For Cast Iron it is recommended to use q=0.2

## Slide 17: Neuber Constants,
Steel Loaded in Tension
Annealed Aluminum
Hardened Aluminum
Sut (ksi) | 15 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90
Sut (Msi) | 103 | 138 | 207 | 276 | 345 | 414 | 483 | 552 | 621
 | 0.175 | 0.380 | 0.278 | 0.219 | 0.186 | 0.162 | 0.144 | 0.131 | 0.122
Sut (ksi) | 10 | 15 | 20 | 25 | 30 | 35 | 40 | 45
Sut (Msi) | 69 | 103 | 138 | 172 | 207 | 241 | 276 | 310
 | 0.500 | 0.341 | 0.264 | 0.217 | 0.180 | 0.152 | 0.123 | 0.111
Sut (ksi) | 50 | 60 | 70 | 80 | 90 | 100 | 120 | 140 | 160 | 180 | 200 | 220 | 240
Sut (Msi) | 345 | 414 | 483 | 552 | 621 | 689 | 827 | 965 | 1103 | 1241 | 1379 | 1517 | 1655
 | 0.130 | 0.108 | 0.093 | 0.080 | 0.070 | 0.062 | 0.049 | 0.039 | 0.031 | 0.024 | 0.018 | 0.013 | 0.009

## Slide 18: Notch Sensitivity Curves Reverse Bending/Axial

## Slide 19: Additional Notch Sensitivity Curves

## Slide 20: ke - Reliability
Reliability, R | Standardized Variable, zR | kc
0.50 | 0 | 1.000
0.90 | 1.288 | 0.897
0.95 | 1.645 | 0.868
0.99 | 2.326 | 0.814
0.999 | 3.091 | 0.753
0.999 9 | 3.719 | 0.702
0.999 99 | 4.265 | 0.659
0.999 999 | 4.753 | 0.620
0.999 999 9 | 5.199 | 0.584
0.999 999 99 | 5.612 | 0.551
0.999 999 999 | 5.997 | 0.520

## Slide 21: Fatigue Terminology
Stress
  σmax, σmin
  σm, σa
  σr
CYCLE
STRESS
NUMBER OF CYCLES

## Slide 22: σm-σa Diagrams for Axial and Bending Loads

## Slide 23: σm-σa Diagrams, A Closer Look Modified Goodman Diagram
Sy
Se
σm
σa
Sy
Su
Sy
0

## Slide 24: 2024 Al

## Slide 25: 7075 Al

## Slide 26: Steel

## Slide 27: Fatigue Failure Due to Combined Stresses
Distortional Energy Method
  Mean von Mises Stresses
  Alternating von Mises Stresses

## Slide 28: Fluctuating Stress Due to Bending and Torsion

## Slide 29: Fluctuating Stress Due to Bending and Torsion

## Slide 30: von Mises Equivalent Stresses

## Slide 31: Factor of Safety: Three Interpretations
Sy
Se
σ’m
σ’a
Sy
Su
A
B
C
D
E
F
Q
P
R
N
σa
σm
N – Normal Point, Normal Operating Load
Q,P,R – Three interpretations of anticipated design overload points

## Slide 32: Using Modified Goodman

## Slide 33: Example
A bar of steel has Su=700MPa, Sy=500MPa, and a fully corrected endurance limit of S3=200MPa. For each case below find the factor of safety which guards against static and fatigue failures.
1.
2.
3.
4.